

[image: ][image: ]

[image: ]     
	TECHNICAL PRODUCT INFORMATION



	Product:
	Green/White film 

	Catalog Number:
	E1914

	UV Resistance:
	3 years at 120KLy 

	Thickness:
	150-300 µ

	Width:
	Up to 18.0m

	Length:
	According to customer order




	Product properties

	Property
	Test Method
	Units
	Value

	Tensile Strength at break[MD]
	ASTM D-882
	MPa.
	25

	Tensile Strength at break[TD]
	ASTM D-882
	MPa.
	25

	Elongation at break [MD]
	ASTM D-882
	%
	650 min

	Elongation at break [TD]
	ASTM D-882
	%
	650 min

	Falling Dart Impact
	ASTM D-1709
	gr.
	700 min

	Total light transmission
	EN13206
	%
	<10%

	Thickness average
	EN13206
	%
	±5% on nominal

	Thickness tolerance
	EN13206
	%
	±15%
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Use and limitation:


· Exposure to chemicals: exposure of greenhouse films to severe chemical conditions has an adverse effect on the lifetime of the film. Avoid excessive use of agrochemicals such as pesticides, herbicides, fungicides and fertilizers. Take measures to prevent direct contact of chemicals to the film. Ensure that metal structures are galvanized and are free from corrosion. When wooden structure parts are used, avoid contact of the film with resin, oil, petroleum or volatile preservatives. Prevent contact of the film with PVC accessories. Chemicals containing halogens, sulfur, copper, iron, are known to accelerate the degradation of greenhouse films.

Specifically, if the following elements are found at levels higher than specified, the films are excluded from this warranty:

Sulfur: max 500 ppm,  Chlorine:  50 ppm, Iron: 50 ppm 

· Overheating: the film has an adverse effect on its lifetime. Hot air should be directed away from the film.

· Disinfection chemical use: when chemicals are used to disinfect the soil, the treated soil must be covered with a film for a minimum of three weeks. After the film is removed, the greenhouse should be ventilated.
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